DRAFT NBS Specification

(not compatible with all design solutions)   screw fastened to wooden battens.

(Suspended Ceiling System)

K40

135	SUSPENDED CEILING SYSTEM

- Please refer to Architect’s drawings ……………………. for locations

- Structural soffit: ………………………

- Ceiling system manufacturer/supplier: Troldtekt A/S, Sletvej 2A, 8310 Tranbjerg J, Denmark Tel: +45 8747 8100 Fax +45 8747 8111 Email: sales@troldtekt.co.uk

- Product reference: Troldtekt® design solutions

- Panel size

- 600 x 1200 mm (Troldtekt® line, Troldtekt® tilt line, Troldtekt® v-line)

- 600 x 1200 mm (Troldtekt® dots, Troldtekt®  curves)

- 600 x 1190 mm (Troldtekt® line design)

- 600 x 1039 mm (Troldtekt® rhombe, Troldtekt® rhombe hatch)

- 600 x 692 mm (Troldtekt® rhombe mini, Troldtekt® rhombe hatch mini)

- 600 x 600 mm (Troldtekt® tiles, Troldtekt® puzzle)

- Thickness: 25mm (only Troldtekt® v-line), 35mm

- Panel finish: FUTURECEM natural grey / Natural wood / Standard colors (White 101 / Grey 202 / Grey 208 / Black 207 / Clay 210) special colors

- Structure: Ultrafine 1mm

- Edge design:

- Troldtekt® line

- Troldtekt® line design

- Troldtekt® v-line

- Troldtekt® tilt line

- Troldtekt® dots

- Troldtekt® curves

- Troldtekt® rhombe / rhombe hatch

- Troldtekt® rhombe mini / rhombe hatch mini

- Troldtekt® tiles

- Troldtekt® puzzle

- Ceiling type: Fine fibre wood wool panels meeting EN 13168 and EN 13964 standards. The panels must be available as PEFC (PEFC/09-31-030) - and FSC® (FSC® C115450)-certified.

- Certified “Gold” Cradle to Cradle” and the "Allergy Friendly Product Award" - "Allergy UK".

- Supports: Wooden battens, minimum size 22X95mm, with a centre spacing of 600mm (Troldtekt® rhombe / rhombe hatch: 300mm).

- Ceiling module: 600X600mm, 600X1200mm, special modules

- Access: All panel units are screw fastened and demountable

- Manufacturer’s Troldtekt components to include Troldtekt self-tapping screws.

- Insulation:	30 or 50mm stone wool (45kg/m3) acoustic pads (If required to complete the required Absorber Class ceiling system).

375 INSTALLING PANEL CEILING SYSTEM

- Installation should be in accordance with manufacturer’s instructions, see www.troldtekt.co.uk  for download.

- Moisture content of boards at time of fixing: Appropriate to end use.

- It is important that the Troldtekt panels are allowed to acclimatise prior to installation. Acclimatisation means that the panels must adapt to the temperature and humidity in the room where they are to be installed.

- Troldtekt panels to wooden battens installed in broken bond

- Cutting: Cut panels neatly and accurately in accordance with manufacturer’s instructions.

- Fixing: Screw fasten panels using Troldtekt prepainted screws securely and firmly to wooden battens.

- Screws are to be positioned carefully, not less than 20/25mm from the panel edges and equally and accurately positioned to one another in accordance with Installation Instructions.

- Provide a flat surface free from bowing and lipping. Set screw heads below surface of boards avoiding overtightening.

- Place 30 or 50mm stone wool acoustic pads over Troldtekt panels and fit tightly between the wooden battens, trimming where necessary.

- Exposed board edges are to be site painted with Troldtekt Touch-up Paint.

395 INTEGRATED SERVICES

- General: Position services accurately, support adequately. Align and level in relation to the ceiling and suspension system. Do not diminish performance of ceiling system.

- Small fittings: Support with rigid backing boards or other suitable means. Do not damage or distort the ceiling.

- Surface spread of flame rating of additional supporting material: Not less than ceiling material.

- Services outlets:

- Supported by ceiling system: Provide additional hangers.

- Independently supported: Provide flanges to support or trim ceiling system.